Armoured Force Cruiser

Vehicle may not be exactly as illustrated

European Level B6 – NIJ Level III

Standard Vehicle Specifications

Engine

- Turbo Diesel- 3250 FTI

- 5 Cylinder, 4 Stroke, Vertical Inline DI (Diesel fuel tank capacity 63ltrs)

- Max Output 100bhp (ISO) @ 3200 RPM

- Max Torque 265 Nm. @ 1800-2000 RPM

- Sump capacity 7.5 Ltrs

Transmission

- G1 18/5 5 speed

- Gear lock synchromesh on forward gears

- 5 forward, 1 reverse

- Single plate, dry friction, hydraulically actuated ,240mm

Suspension & Brake System

- Independent torsion bar with hydraulic telescopic shock absorbers & anti roll-bar

- Rear semi elliptical leaf springs with hydraulic telescopic shock absorbers

- Hydraulic dual circuit with front solid disc brakes & rear drum brake

Dimensions & Gross Vehicle Weight

- Overall width 1660

- Overall length 4832

- Overall height 2055

- Min. Ground Clearance 225

- Gross Vehicle weight 3620kg approx(This includes armor)

Unique Features

- Air Conditioning

- Power assisted steering

- 16” Steel wheel rims

- 6mm Tubular ladder chassis frame

- Turning Radius 7.0 mtrs

- Four wheel drive (4x4)

Specifications of Armor & Vehicle Alterations

- Five sided armoring of passenger cabin to give maximum protection against 7.62 x 51mm & 5.56 x 45mm

- A, B, C & D pillars are protected with armor, as are front fenders, (wings) rear wheel arches & firewall. This adds structural rigidity to the overall vehicle, floor is fitted with the same steel as the sides, roof will protect against 90 degree angle shots.

- All passenger doors are fitted with overlap system and antispall guard which provides maximum strength retention to prevent penetration through door posts & pillars.

- Vehicles armor plates are stitch-welded using high-intensity MIG welders. This process ensures the structural integrity is uncompromised by thermal and chemical variations of the material.

- The glass is installed using ballistic grade steel frame for added protection which gives extra support to help prevent cracks & fractures. This also provides added protection for these potentially weak areas.

- The hinges are bolted directly onto the armor through the pillars & the doors to prevent stress on the hinges and the internal panels which otherwise will lead to cracking under the extra weight.

Transparent Armor

- Flat glass, PVB/polycarbonate laminate 6.2kgs./sq.ft(13.7lbs/sq.ft) – Thickness is 39mm (Replaces all OEM glass).

- Glass is manufactured under strictly controlled conditions, using only the highest grade materials.

- Anti-Spall shield protects against glass splinters, chemical attacks. Autoclave temperature allows the polycarbonate to lose its memory to prevent delaminating & internal stress. The glass also provides multi hit protection.

- The ballistic performance of bullet resistance glass can be diminished when the glass is exposed to high temperatures; Solar Plus ensures total ballistic resistance performance for a longer period of time.

- Glass is tested in accordance with EN 1522 & EN 1063 European Level B6 – NIJ Level III

Ballistic Protection Level Details

(Please refer to Class VR6 for this vehicle)

Standard Vehicle Features

- Seating for nine persons (including the driver)

- Runflat devices fitted in all five wheels.

- Fuel tank & water separator encased with ballistic steel to protect against explosive projectiles.

- All five passenger doors are fitted with heavy duty webbed door straps to prevent fouling.

- Battery is protected within an armored box in the engine compartment.

- Front fenders (wings) L/H & R/H armoured to protect against side shots

- Exhaust protection installed to prevent foreign objects being inserted.

- Suspension is reinforced or modified as necessary to compensate for the additional weight.

- Gun-ports are installed on both L/H & R/H quarter window & the rear barn door

- Fire extinguisher installed inside cabin

- V-Trac system installed as standard